UK/SC/3621 Issue 5
Specification for

INCISED CAMOUFLAGE GARNISHING
DESERT
[image: image1.png]



OPERATIONAL INFRASTRUCTURE

PROGRAMME
Property of:

OIP
DE&S

MOD Abbey Wood

NN/239/042
Date of Approval: 24 Sept 2013
NV/318/05
Date of Previous Issue: 30 July 2002
NATO Stock Numbers
Pattern No.
1080-99-797-1070
Desert
1186
IPR STATEMENT

This specification contains information which is proprietary to the Secretary of State for Defence and shall remain the property of the Secretary of State. It is issued in strict confidence and must not be seen by any unauthorised person. The specification is supplied solely for the purpose of Information/Tender/Contract and shall not be copied or reproduced or used for any other purpose whatsoever without the express prior written permission of the Secretary of State as represented by the Intellectual property rights group.

Technical data in this document refers to the edition current at the date of tender or contract unless otherwise stated.

CROWN COPYRIGHT RESERVED

SPECIFICATION UK/SC/3621 - ISSUE TABLE

	Issue Number
	Comments
	Date

Published

	1
	Initial issue
	8 April 1970

	2
	Amendment 1
	24 Sept 1986

	3
	Specification reformatted.  Standards updated.  Amendment 1 deleted.
	30 July 2002

	4
	Specification reformatted.
	28 July 2010

	5
	Reformatted.  Snow and urban patterns deleted.  Reference to Harrier concealment set deleted.  Packaging clause standardized across all garnish.  Annex A deleted.
	24 Sept 2013


1 SCOPE

1.1 This specification governs the incising of polyurethane coated nylon fabric used as garnishing for Snow, Desert and Urban camouflage nets.
2 RELATED SPECIFICATIONS AND DOCUMENTS

Reference is made in this specification to:

2.1 Standards

UK/SC/4880
Cloth, coated, polyurethane on nylon (Beige/Light Brown) IRR
DEF STAN 93-116
Polyethylene (Low density) film for packaging types 1, 2 and 3
2.2 Drawings

D3341
Incising, Pattern MOD S3
2.3 Reference in this specification to a British Standard or any other specification or document means, unless otherwise stated, the edition current at the date of such tender or contract.

3 SAMPLES
3.1 If requested by the Contractor reference samples of the materials will be provided by the Authority.  They are to provide the criteria for any particulars or properties not fully defined in this specification.

4 MATERIALS

4.1 Cloth, coated polyurethane on nylon, beige/light brown, IRR shall be to Specification UK/SC/4880, Pattern No.1186.
5 MANUFACTURE

5.1 The fabric shall be incised full width in accordance with the drawing quoted in Para 2.2 above.

5.2 The incisions shall be made so that all the cuts in the fabric have clean edges.  There shall be no imperfect incisions.

5.3 If more than one layer of fabric is incised at one operation, each layer of the incised fabric shall be capable of being separated easily and without damage.

5.4 No artificial heat shall be used to assist the incising of the material.

5.5 The material shall remain in the length supplied and 1.37 metre width, no cutting will be permitted.

6 PACKAGING

6.1.1 Rolls shall be delivered in a clean condition suitably wrapped in black polythene to DEF-STAN 93-116, 250 µm gauge.  Rolls shall be sealed with adhesive tape.  Each roll shall have full marking on a label attached to the outside of the roll.  Rolls shall NOT be cut into lengths, incising shall be continuous throughout.

6.1.2 Other packaging (preservation, identification and packing) is to be in accordance with the terms of the contract.

7 INSPECTION

7.1 Inspection shall be carried out to the satisfaction of the Authority.
1 OF 4

