|  | # Performance Specification |
| --- | --- |

Excerpt from NML’s Performance specification for Display cases

1.1	Materials – General Considerations

1.2	All materials to be durable and maintainable.

1.3	All materials to be inert and stable, proven for safe contact with objects without releasing corrosive or tarnishing vapour.  All materials for case interiors to be selected from NML’s approved list where possible.  For any other materials not on the list, product data, samples (if required) and documented proof of material being passed ‘Permanent’ by Oddy Testing to be supplied to NML for evaluation. 
Oddy Tests take a minimum of 4 weeks for a result. As some materials can fail material testing, alternatives require selecting and further testing may be required, the programme must take this time requirement into account.

1.4	Safety data sheets for all materials used should be approved by NML prior to manufacture.

1.5	Minimum periods required for curing/off-gassing before installation of any materials into case:

- adhesives						4 weeks

- glazing, water based paints + varnishes		2 weeks

- sealants						1 week

2. 	Case Plinths

2.1	NML approves of three primary methods of interior construction:

- Forrex™ or Foamalux™ PVC rigid board, minimum thickness of 19mm for load bearing and structural requirements and in agreement with NML. Fabric should be fixed using approved tapes and/or staples may be used. Only tapes and adhesive film currently approved may be used (see Approved Tapes below). Where paints are used, as agreed with NML (see Display Case Schedule) these should be approved water based emulsion paints applied to a pre-“keyed” surface. Only primers approved by NML be used, where these are appropriate, for use on  Forrex™ or Foamalux™ PVC rigid board and approved ‘Permanent’ by Oddy Testing and in agreement with NML

- Formaldehyde free MDF (e.g. ZF MDF) covered with a heat-sealed barrier film such as Moistop, wrapped with NML approved fabric or coated with four coats of Dacrylate™ (or agreed alternative) water based (non-V.O.C. emitting) acrylic lacquer. Fabric should be fixed using approved tapes, and the barrier film over ZF MDF should not be punctured i.e. fabric should not be stapled. Tapes and adhesive film currently approved include:

Approved Tapes:

- Gudy 870 transfer adhesive

- Lomacoll double-sided mounting adhesive

- 3M 415 double-sided tape

- 3M 425 Scotch aluminium adhesive tape

2.2	Dibond, Lucabond or Hexlite may be used in certain circumstances, after prior approval from NML.

2.3	A sample of the plinth should be provided to NML at the outset of contract for 	approval.